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SECTION 09930
HARDWOOD FLOOR ADHESIVES, FINISHING AND MAINTENANCE
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** NOTE TO SPECIFIER ** Bona US; wood floor adhesives, finishing and maintenance products.
This section is based on the products of Bona US, which is located at:
24 Inverness Place E. Suite 100
Englewood, CO 80112
Toll Free Tel: 800-872-5515
Tel: 303-371-1411
Fax: 303-307-5029
Email:request info (usadmin@bona.com)
Web:https://www.bona.com
[Click Here] for additional information.
For architects and designers across the globe Bona has provided professionals with premium products and systems developed to maintain the natural beauty of hardwood floors. Each and every Bona product works in tandem to create perfect floors every time. With a century of experience innovating, studying and perfecting the Bona System we stand behind everything that we do.
PART  1   GENERAL
SECTION INCLUDES
Hardwood floor adhesives, finishing and maintenance of the following types:
Penetrating oil finishes.
RELATED SECTIONS
** NOTE TO SPECIFIER ** Delete any sections below not relevant to this project; add others as required.
Section 09640 - Wood Flooring.
REFERENCES
** NOTE TO SPECIFIER ** Delete references from the list below that are not actually required by the text of the edited section.
ASTM International (ASTM):
ASTM D2047 - Standard Test Method for Static Coefficient of Friction of Polish-Coated Flooring Surfaces as Measured by the James Machine.
ASTM E492 - Standard Test Method for Laboratory Measurement of Impact Sound Transmission Through Floor-Ceiling Assemblies Using the Tapping Machine.
ASTM F1869 - Standard Test Method for Measuring Moisture Vapor Emission Rate of Concrete Subfloor Using Anhydrous Calcium Chloride.
ASTM F2170 - Standard Test Method for Determining Relative Humidity in Concrete Floor Slabs Using in situ Probes.
SUBMITTALS
Submit under provisions of Section 01300.
Product Data: Manufacturer's data sheets on each product to be used, including:
Preparation instructions and recommendations.
Storage and handling requirements and recommendations.
Installation methods.
** NOTE TO SPECIFIER ** Delete selection samples if colors have already been selected.
Selection Samples: For each finish product specified, two complete sets of color chips representing manufacturer's full range of available colors and patterns.
Verification Samples: For each finish product specified, two samples, minimum size 6 inches (150 mm) square, representing actual product, color, and patterns.
QUALITY ASSURANCE
Installer Qualifications: Trained in application of the manufacturer's floor products.
** NOTE TO SPECIFIER ** Include a mock-up if the project size and/or quality warrant taking such a precaution. The following is one example of how a mock-up on a large project might be specified. When deciding on the extent of the mock-up, consider all the major different types of work on the project.
Mock-Up: Provide a mock-up for evaluation of surface preparation techniques and application workmanship.
Finish areas designated by Architect.
Do not proceed with remaining work until workmanship, color, and sheen are approved by Architect.
Refinish mock-up area as required to produce acceptable work.
DELIVERY, STORAGE, AND HANDLING
Store products in manufacturer's unopened packaging until ready for installation.
Store and dispose of solvent-based materials, and materials used with solvent-based materials, in accordance with requirements of local authorities having jurisdiction.
PROJECT CONDITIONS
Maintain environmental conditions (temperature, humidity, and ventilation) within limits recommended by manufacturer for optimum results. Do not install products under environmental conditions outside manufacturer's limits.
PART  2   PRODUCTS
MANUFACTURERS
Acceptable Manufacturer: Bona US, which is located at: 24 Inverness Place E. Suite 100; Englewood, CO 80112; Toll Free Tel: 800-872-5515; Tel: 303-371-1411; Fax: 303-307-5029; Email:request info (usadmin@bona.com); Web:https://www.bona.com
Requests for substitutions will be considered in accordance with provisions of Section 01600.
PENETRATING OIL FINISHES
** NOTE TO SPECIFIER** Bona Craft Oil 2K is a highly versatile unique blend of different vegetable oils, modified for superior impregnation and long-lasting protection of wood floors. The exclusive blend is low in odor, easy to handle and gives you the option of top coating with Bona Traffic HD, Traffic or Traffic Naturale. The formulation is environmentally responsible, containing very low solvents (less than 4 percent) allowing for total saturation. Suitable for hardwood floors in residential and commercial environments.
Extremely high degree of saturation.
Rapid drying (ready for light use in 8 hours) and easy to apply.
Low solvent content and low odor.
Easy repair and blending.
Unlimited color palette.
Overcoatable with Bona Traffic HD, Traffic or Traffic Naturale.
GREENGUARD certified for indoor air quality.
Premium Commercial Penetrating Hardwood Floor Finish:
Product: Bona Craft Oil 2K as manufactured by Bona US.
Ingredients: Pigments, oil-modified polyurethane resin, vegetable oil, petroleum distillates, and driers.
Color: Neutral.
Color:  Charcoal.
Color:  Frost.
Color:  Ash.
Color:  Clay.
Color: Air.
Color: Pebble.
Color: Sand.
Clarity: Transparent color.
Solids: 96 to 98 percent (depending on color).
US Regulatory VOC Compliant: 25 g/L (0.21 pounds per gallon).
Dilution: Do not dilute.
Odor: Non-offensive odor.
Drying Time: Light use: 12 to 24 hours (8 hours Neutral/12 hours colors).
Cure Rate, 24 Hours:  70 percent. Cure Rate, 5 Days:  100 percent.
Stability: 2-year shelf life in unopened container.
Cure Time:  100 percent cured after 7 days.
Certification: GREENGUARD Certified for indoor air quality.
PART  3   EXECUTION
EXAMINATION
Do not begin installation until substrates have been properly prepared.
If substrate preparation is the responsibility of another installer, notify Architect of unsatisfactory preparation before proceeding.
Building climate control system shall be functioning with a temperature of 65 to 80 degrees F (18.3 to 26.7 degrees C) and maximum relative humidity of 70 percent for 72 hours before flooring is installed, during installation, and for 72 hours after installation. Acclimate flooring according to manufacturer's instructions.
PREPARATION
Protection: Protect adjacent finish surface to prevent damage during sanding and finish system application.
Substrate:  Must be clean, smooth, dry, free of loose material and structurally sound, with the surface slightly textured for best adhesion (similar to a light broom finished concrete).
Remove adhesive residue, paint, concrete curing compounds or other contaminants that may affect adhesive bond. Abrasive blasting, shot blasting or scarifying may be necessary to completely remove some of these residues.
Surface cracks, grooves, depressions, control joints or other non-moving joints, and other irregularities must be filled or smoothed with a Portland Cement-based patching and/or leveling compound.
Levelness:  To 3/16 inch (5 mm) in a 10 ft (3048 mm) span. If the concrete slab is to be leveled, primer/sealer shall be applied to the slab prior to application of the leveling compound.
Slab Temperature:  55 to 95 degree F (12.8 to 35 degrees C).
Other suitable substrates include wood and radiant heat flooring (refer to manufacturer's recommended installation instructions).
MOISTURE TESTING
Concrete Floors:
Concrete Slabs:  Conduct moisture testing per ASTM F1869 and/or  ASTM F2170.
Primer/Sealer:  Two coats prior to installation of hardwood flooring with an adhesive when MVER using ASTM F1869 (Calcium Chloride test) exceeds 12 lbs per 24 hrs per 1000 sq ft (5.86 kg per 24 hrs per 100 sq m) or when using ASTM F2170 (RH probe test) exceeds 85 percent relative humidity.
Moisture Content:  Should not exceed 18 lbs per 24 hrs per 1000 sq ft (8.79 kg per 24 hrs per 100 sq m) or 95 percent relative humidity.
When using a Tramex measuring device to identify moisture levels in cementitious based substrates, use the Tramex measuring device to find the highest reading in the area to be installed and then run the concrete moisture testing method at the location of the recorded highest reading.
As a general guideline for floors with no in-floor heating system, if the Tramex is below 4 percent, primer/sealer will not be necessary; if between 4 and 6 percent, primer/sealer is required.
Wood Subfloor:
For moisture content and quality of substrates, the guidelines of the wood floor manufacturer shall be followed.
Wood Subfloor Moisture Content:  20 percent maximum.
** NOTE TO SPECIFIER **  Delete if not required.
SANDING AND PREPARATION OF NEW FLOORS:
Sand and prepare floor using accepted industry association methods.
Vacuum thoroughly.
Stained Floors:  Make final cut with 80 to 100 grit paper. Then MultiDisc with 80 to 120 grit paper.
Unstained Floors:  Make final cut with 80 to 120 grit paper. Then MultiDisc with 120 to 150 grit paper. This burnishing will reduce the amount of grain raise.
Use a Tampico Brush on a buffer and vacuum thoroughly.
Tack with a dry Bona Microfiber Tacking Pad or cloth to remove dust.
Apply finish system.
FINISH APPLICATIONS, GENERAL
** NOTE TO SPECIFIER ** For new installation of floors, use only in structures with humidity and temperature controls. Do not use over channel and clip floor systems in environments not controlled for temperature and humidity. Delete if not required.
Comply with instructions and recommendations of floor finish system manufacturer.
Finish System:  As scheduled or indicated on the drawings.
PENETRATING OIL FINISHES APPLICATIONS
Mixing:
Using a hammer, drive a screwdriver through top and bottom of upper container (Part B) and allow hardener to completely empty into bottom container (Part A).
Remove lid and mix content thoroughly. Do not thin.
To mix smaller amounts of Bona Craft Oil 2K, use a 1:9 ratio.
Bona Craft Oil 2K cannot be rehardened.
Pot Life:  Must be used within 6 to 8 hours after mixing.
Application:
Coverage Rate:  0.33 gallons (1.25 Liters)per 600 to 800 sq ft (55.74 to 74.32 sq m) of wood flooring. Rate varies depending on wood species and sanding sequence.
Apply thin coat of mixed Bona Craft Oil 2K to floor using a 175 rpm buffer and a red buffing pad working back and forth with the grain of the wood when possible.
For areas the buffer cannot reach, use a trowel or a cut-in pad to apply.
Allow oil to penetrate wood surface for 15 to 30 minutes.
Remove excess oil using a buffer and a clean, Bona Cotton Cloth wrapped around a 1 inch (25 mm) white, red or green buffing pad. Change cloth as needed.
Drying:  Allow oil to dry thoroughly before use.
Neutral:  8 hours.
Colors:  12 hours.
Recommended Conditions:  65 to 80 degrees F (18.3 to 26.7 degrees C), 40 to 60 percent relative humidity.
High humidity and/or low temperature conditions extend dry time.
Increased ventilation and airflow reduce dry time.
Cure Time:
Walkable:  8 to 12 hours but remains susceptible to scuffing or marring until completely cured.
Ready for light use and furniture placement:  12 to 24 hours
Full Cure:  5-7 days.  Recommended Conditions:  65 to 80 degrees F (18.3 to 26.7 degrees C), 40 to 60 percent relative humidity.
Do not replace area rugs until the floor has fully cured.
Top Coating:  In situations where an additional layer of protection is desired.
Bona Craft Oil 2k can be top-coated with Bona Traffic HD, Bona Traffic or Bona Traffic Naturale.
Apply Bona Craft Oil 2K  and allow to dry per manufacturer's instructions and this specification.
Vacuum and tack the floor with a dry Bona Microfiber Tacking Pad.
Apply 1 to 2 coats of Bona Traffic HD, Bona Traffic or Bona Traffic Naturale per label instructions.
After Fully Cured:
Deep clean floor using PowerScrubber and Bona Deep Clean Solution.
Allow adequate time for surface to dry completely.
Apply the same color Craft Oil 2K to the floor per the directions and allow to dry completely (8 hours for Neutral and 12 hours for all other colors).
Vacuum and tack the floor with a dry Bona Microfiber tacking pad.
Apply Bona Traffic HD, Bona Traffic or Bona Traffic Naturale per label instructions.
Be sure floor is free from wax, polish and oily residues.
Adhesion failure can occur if these recoating processes are not followed and the floor has not been tested for compatibility.
PROTECTION
After application, protect floor finish from damage during subsequent work.
Do not allow foot traffic until floor is sufficiently dried and cured.
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