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** NOTE TO SPECIFIER ** Bona US; wood floor finishing and maintenance products.
.
This section is based on the products of Bona US, which is located at:
24 Inverness Place E. Suite 100
Englewood, CO 80112
Toll Free Tel: 800-872-5515
Tel: 303-371-1411
Fax: 303-307-5029
Email: request info (usadmin@bona.com)
Web: https://www.bona.com  
 [ Click Here ] for additional information.
At Bona we are committed to the whole lifetime of hardwood floors. We are devoted to providing solutions that keep a floor perfect during its entire life. Through our long commitment and constant search for innovation we are able to offer lasting, sustainable results for professionals and floor owners. With Bona you can expect a commitment that lasts for generations.
Today Bona is a world leading innovator with a unique system, having local presence all across the world. Since established in 1919 we are now, through subsidiaries and distributors, present in more than 50 different countries all over the world. .
PART  1   GENERAL
1.1  SECTION INCLUDES
A.  Hardwood athletic floor finishing and maintenance of the following types:
1.  Athletic floor finish.
2.  Athletic floor maintenance.
3.  Waterborne sealers. 
1.2  RELATED SECTIONS
** NOTE TO SPECIFIER ** Delete any sections below not relevant to this project; add others as required.
A.  Section 09 64 00 - Wood Flooring.
1.3  SUBMITTALS
A.  Submit under provisions of Section 01 30 00 - Administrative Requirements.
B.  Product Data: Manufacturer's data sheets on each product to be used, including:
1.  Preparation instructions and recommendations.
2.  Storage and handling requirements and recommendations.
3.  Installation methods.
** NOTE TO SPECIFIER ** Delete selection samples if colors have already been selected.
C.  Selection Samples: For each finish product specified, two complete sets of color chips representing manufacturer's full range of available colors and patterns.
D.  Verification Samples: For each finish product specified, two samples, minimum size 6 inches (150 mm) square representing actual product, color, and patterns.
1.4  QUALITY ASSURANCE
A.  Installer Qualifications: Trained in application of the manufacturer's floor products.
** NOTE TO SPECIFIER ** Include a mock-up if the project size and/or quality warrant taking such a precaution. The following is one example of how a mock-up on a large project might be specified. When deciding on the extent of the mock-up, consider all the major different types of work on the project.
B.  Mock-Up: Provide a mock-up for evaluation of surface preparation techniques and application workmanship.
1.  Finish areas designated by Architect.
2.  Do not proceed with remaining work until workmanship, color, and sheen are approved by Architect.
3.  Refinish mock-up area as required to produce acceptable work.
1.5  DELIVERY, STORAGE, AND HANDLING
A.  Store products in manufacturer's unopened packaging until ready for installation.
B.  Store and dispose of solvent-based materials, and materials used with solvent-based materials, in accordance with requirements of local authorities having jurisdiction.
1.6  PROJECT CONDITIONS
A.  Maintain environmental conditions (temperature, humidity, and ventilation) within limits recommended by manufacturer for optimum results. Do not install products under environmental conditions outside manufacturer's absolute limits.
PART  2   PRODUCTS
2.1  MANUFACTURERS
A.  Acceptable Manufacturer: Bona US, which is located at: 24 Inverness Place E. Suite 100; Englewood, CO 80112; Toll Free Tel: 800-872-5515; Tel: 303-371-1411; Fax: 303-307-5029; Email: request info (usadmin@bona.com); Web: https://www.bona.com 
B.  Requests for substitutions will be considered in accordance with provisions of Section 01 60 00 - Product Requirements.
** NOTE TO SPECIFIER ** Our Athletic Floor Care (AFC) finishes are the top athletic finishes in the industry for durability and appearance. The premium products within our portfolio are specifically formulated to meet all federal and state clean air quality standards and are for professional use on maple athletic floors. Delete if not required.
2.2  WATERBORNE SEALERS 
A.  Sealers: 
** NOTE TO SPECIFIER **  Bona SuperSport DTS is a specially formulated waterborne sanding sealer for use with all Bona waterborne finishes. Bona SuperSport DTS seals the wood; develops a deep natural tone, vibrant look; abrades easily; and prevents the finish from penetrating into the wood surface. 
1.  Product: Bona SuperSport DTS as manufactured by Bona US. 
a.  Ingredients: Water, polymeric resin, silica derivate, diethylene glycol monoethyl ether, propylene glycol. 
b.  Color: Milky white (wet). 
c.  Clarity: Clear when dry. 
d.  pH: 7.5 to 7.9. 
e.  Solids: 31 to 32 percent. 
f.  Density: 8.66 lbs./gallon (1.04 S.G.). 
g.  US Regulatory VOC: 250 g/L. 
h.  Odor: Non-offending. 
PART  3   EXECUTION
3.1  MANUFACTURER'S INSTRUCTIONS
A.  Comply with the instructions and recommendations of the floor finish system manufacturer.
B.  For new installation of floors, use only in structures with humidity and temperature controls. Do not use over channel and clip floor systems in environments not controlled for temperature and humidity.
3.2  EXAMINATION
A.  Do not begin installation until substrates have been properly prepared.
B.  If substrate preparation is the responsibility of another installer, notify Architect of unsatisfactory preparation before proceeding.
3.3  PREPARATION
A.  Protection: Protect adjacent finish surface to prevent damage during sanding and sport floor system application.
3.4  APPLICATION
A.  Specific application methods vary with product. Consult manufacturer and comply fully with manufacturer's application recommendations.
1.  Before using these products, read and understand all directions and the Material Safety Data Sheets (MSDS).
2.  Shake well before using.
3.  Do not thin products.
4.  Keep from freezing.
B.  Finish System: As scheduled or indicated on the drawings.
** NOTE TO SPECIFIER ** Edit system to comply with Bona waterborne sealer and finish system selected.
1.  4-coat system, 1 to 2 coats of a sport sealer, court lines paint (where scheduled or indicated) and 2 to 3 coats of a sport court finish.
3.5  PROTECTION
A.  After application, protect floor finish from damage during subsequent work.
B.  Do not allow foot traffic until floor is sufficiently dried and cured.
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